## Slide 1: 28nm

## Slide 2
IDSAT vs stress time, VDS= 2.7V, VGS= 2.2V, W/L = 210nm/60nm
Notes: Short-term recovery every time when consecutive stress stops, correlated with PBTI’s recovery.
Limited effective shift after the first 400ms

## Slide 3
IDSAT vs stress time, VDS= 2.7V, VGS= 2.2V, L = 60nm
IDSAT vs stress time, VDS= 2.7V, VGS= 2.2V, W/L = 210nm/60nm
3σ read current margins
1 cell:

## Slide 4: 16nm

## Slide 5
IDSAT vs stress time, VDS= 2.0V, VGS= 1.8V, L = 36nm, NFIN = 2
Notes: Short-term recovery every time when consecutive stress stops, correlated with PBTI’s recovery.
Limited effective shift after the first 400ms

## Slide 6
IDSAT vs stress time, VDS= 2.7V, VGS= 2.2V, L = 60nm
IDSAT vs stress time, VDS= 2.0V, VGS= 1.8V, L = 36nm, NFIN = 2
1 cell:
1 month retention
(room temperature)